# TECHNICAL DATASHEET

### HQN PU PORESEALER

Product Code: HQN PU PS

## Product Description

HQN PU Poresealer is a high-performance polyurethane-based sealing compound designed to penetrate and seal porous substrates. It improves surface integrity, reduces absorption, and prepares the substrate for subsequent coating systems.

## Key Features

- Excellent penetration into porous surfaces

- Effectively reduces surface porosity

- Improves adhesion of subsequent coatings

- Enhances surface strength and durability

- Easy to apply

- Fast curing

## Recommended Use

- Sports Flooring

## Application Method

- Ensure the surface is clean, dry, and free from dust, oil, and loose particles

- Apply using roller, brush, or spray equipment

- Allow proper penetration into the substrate

- Apply a second coat if required depending on surface porosity

## Technical Properties

| Property | Value |
| --- | --- |
| Appearance | Clear / Slightly Amber Liquid |
| Base | Polyurethane |
| Application Temperature | 10°C – 45°C |
| Drying Time | 4 – 8 hours (depending on conditions) |

## Coverage

- Approx. 0.5 - 1 kg/m² per coat
(depending on surface porosity)

## Shelf Life

- 6 Months

## Storage

- Store in a cool, dry place

- Keep away from direct sunlight and moisture

- Keep container tightly closed when not in use

## Safety & Handling

- Use appropriate PPE (gloves, mask, goggles)

- Ensure adequate ventilation during application

- Avoid contact with skin and eyes

## Disclaimer

The information provided in this datasheet is based on current knowledge and experience. It is the user’s responsibility to ensure the product is suitable for the intended application. The manufacturer is not liable for improper use or application.